GC 8 x 30AW

acid-washed granular activated carbon

GC 8x30AW is a virgin acid washed activated carbon which is granular in form.  Made from the finest grades of bituminous coal and then acid washed, it is ideal for many liquid phase applications including the removal of organics from water streams.  Its superior adsorptive capacity and low level of impurities make it cleaner than most other carbons and gives it longer life expectancy.  NSF certified, it is suitable for drinking water and food grade applications.

Specifications

Mesh Size – 8 X 30, %:	90 (min)

Less than No. 8, %:	5 (max)

Greater than No. 30, %:	5 (max)

Iodine No., mg/g:	900 (min)

Surface Area, m2/g:	900 (min)

Hardness, %:	90 (min)

Moisture Content, % (as packaged):	3.0 (max)

Ash Content, %:	10 (max.)

Typical Density,  lbs./cu.ft.:	29-33

g/cc:	0.47-0.53

pH:	6-7 (avg)

*Standard packaging is in 55 OR 1100 lb. bags.  Other packaging is available upon request.

Caution!

Wet activated carbon removes oxygen from air causing a severe hazard to workers inside carbon vessels.  Confined space/low oxygen procedures should be put in place before any entry is made.  Such procedures should comply with all applicable local, state and federal guidelines.

33 Paterson Street, Paterson, New Jersey 07501  Tel: 973 523 2223  Fax: 973 523 1494

www.generalcarbon.com		sales@generalcarbon.com

# Text boxes

“CLEANING THE WORLD WITH ACTIVATED CARBON”